## Slide 1
Fatigue Characterization of Asphalt Binders with the Linear Amplitude Sweep (LAS)
Cassie Hintz, Raul Velasquez, Hassan Tabatabaee, Hussain Bahia
Updated in 03/19/2019

## Slide 2: Content
Part 1: Binder Fatigue Testing
Part 2: LAS: Theoretical Base
Part 3: Performing the LAS test
  Anton Paar Rheometers
  TA Rheometers
  Bohlin Rheometers
Part 4: Analysis of LAS results

## Slide 3: Binder fatigue testing
PART 1:

## Slide 4: Superpave Bitumen Tests
RV
Rotational
Viscometer
DSR
Dynamic Shear
Rheometer
BBR
Bending Beam Rheometer
DT
Direct
Tension Test
Related to Performance!
Climate -- PG HT-LT
Traffic Speed – DSR
Traffic Volume – PG shift
Traffic loading – NA
Pavement Structure – NA
Assumption:
Bitumen in Linear VE
range
Notes: 4

## Slide 5
Binder Fatigue: Superpave Specification (|G*|·sinδ)
Data from NCHRP 9-10

## Slide 6: Binder Fatigue: Time Sweep (NCHRP 9-10)

## Slide 7: Background – Asphalt Mixture Fatigue
Asphalt mixture fatigue characterization relies on following fatigue law:
  Number of Cycles to Failure = A × (Applied Load)B
MEPDG Model:
where: hac = Total thickness of the asphalt layers
structure
traffic
stiffness / temperature

## Slide 8: Background – Asphalt Fatigue

## Slide 9: Background – VECD
Viscoelastic Continuum Damage (VECD) analysis has been used for asphalt mixtures since the late 1980’s.
Relies on constitutive modeling to determine the deviation of damaged test results from undamaged properties.
Deviation from initial undamaged properties with respect to number of cycles used to calculate damage.
Characteristic plot used to back-calculate fatigue performance under different testing conditions.

## Slide 10: Background – VECD

## Slide 11: Background – Summary
Asphalt concrete has been shown to have a well-defined relationship between loading input and fatigue life.
VECD analysis can be an effective tool to determine damage characteristics.
Conventional binder fatigue procedure (time sweep) is problematic.
Binder fatigue testing needs an efficient procedure that can do more than rank relative performance for a single condition.

## Slide 12: Linear amplitude sweep: theoretical base AASHTO TP101-12
PART 2:

## Slide 13: NewTest Method
Linear Amplitude Sweep
  Employs the DSR and standard geometry
  Systematically increases applied load to accelerate damage
  Strain-controlled to avoid accumulated deformation
  Use of VECD allows for calculation of fatigue life at any strain level

## Slide 14: New Test Method
Frequency Sweep
+

## Slide 15: Background – Asphalt Fatigue

## Slide 16: Fatigue Law Parameter “B”
  B = -2α
  α obtained from frequency sweep
  α can be calculated using the slope of log-log G’(ω) plot
    where G’(ω)=|G*|·cos δ(ω)
  α = 1 + 1/m
    where m is slope of the log-log G’(ω) plot

## Slide 17: Fatigue Law Parameter “A”
Where
  Df = (0.35)(C0 / C1)^(1 / C2)
    Damage at failure: Failure corresponds to a 35% reduction in G*·sinδ
  f = Loading frequency (10 Hz).
  k = 1 + (1 – C2)α
  ID = undamaged complex modulus
C1 and C2 come from curve fit:
  Where D = damage

## Slide 18: Damage Curve
Chart: VECD Damage Curve from Amplitude Sweep

## Slide 19: Parameters C1 and C2
Model can be linearized to determine curve coefficients:
Y = µ + β·x
  C0 is average |G*|·sinδ from the 0.1% strain step
  log(C1) is intercept and C2 is slope of
  log(C0 - |G*|·sinδ) versus log(D(t))
  **IGNORE DATA CORRESPONDING TO D(t) less than 100

## Slide 20: Linearized Damage Curve
Chart: log(Damage)

## Slide 21: Linear amplitude sweep: theoretical base AASHTO TP101-14
PART 2:
Updated part
New Standard
P21-26

## Slide 22: Fatigue Law Parameter “B”
  B = -2α
  α obtained from frequency sweep
  α can be calculated using the slope of log-log G’(ω) plot
    where G’(ω)=|G*|·cos δ(ω)
  α = 1/m
    where m is slope of the log-log G’(ω) plot

## Slide 23: Fatigue Law Parameter “A”
Where
  Df = (C0 – C at Peak Stress/C1)^(1 /C2)
    Damage at failure: Failure corresponds to the reduction in initial G’(ω) at the peak shear stress
  f = Loading frequency (10 Hz)
  k = 1 + (1 – C2)α
C1 and C2 come from curve fit:
  Where D = damage
  C(t)= , which is |G*| at time, t divided by the initial “undamaged”
  value of |G*|

## Slide 24: Damage Curve
Chart: VECD Damage Curve from Amplitude Sweep

## Slide 25: Parameters C1 and C2
Model can be linearized to determine curve coefficients:
Y = µ + β·x
  C0 =1, the initial value of C
  log(C1) is intercept and C2 is slope of
  log(C0 – C (t )) versus log(D (t ))
  **IGNORE DATA CORRESPONDING TO D(t) less than 10

## Slide 26: Linearized Damage Curve
Chart: log(Damage)

## Slide 27: Summary
The LAS test is a DSR procedure consisting of a frequency sweep and strain amplitude sweep
Goal: derive fatigue law
Parameters “A” and “B” are
binder properties
  “A” from amplitude sweep
    Higher A increases fatigue life
  “B” from frequency sweep
    Higher magnitude of B decreases fatigue life (at a constant A)
Traffic
Structure

## Slide 28: Performing the LAS Test: (a) Anton-paar rheometers
PART 3:

## Slide 29: Anton-Paar Rheometers
The test has been successfully tested on the following Anton-Paar Rheometers:
  MCR 300 (Smartpave)
  MCR 301
Direct Strain Oscillation (DSO) module recommended but not required

## Slide 30: Anton-Paar Rheometers
Chart: Time (sec)
 | A | % Difference
With DSO | 8.04E+06 | 
Without DSO | 8.75E+06 | 8.47%

## Slide 31: Anton-Paar Rheometers
Video

## Slide 32: Performing the LAS Test: (b) TA rheometers
PART 3:

## Slide 33: TA Rheometers
Procedure can be run as specified in AR2000 EX
AR2000 at UW does not have capability to conduct procedure exactly as specified but results are not substantially affected
  Cannot allow for 100 cycles of loading per strain exactly (typically includes 120-140 cycles per strain step)
  Cannot generate one point per second (able to obtain approximately one point every three seconds)

## Slide 34: TA Rheometers
Video

## Slide 35: Performing the LAS Test: (b) Bohlin rheometers
PART 3:

## Slide 36: Bohlin
Unable to successfully conduct LAS test in UW’s Bohlin C VOR-200 rheometer
  DSR stops oscillating between strain steps
  Malvern support stated their Kinexus rheometers are capable of running procedure
  Contact with Malvern support revealed there was no solution
    UW’s rheometer requires several seconds to process data between each strain step
    Faster computer will reduce “rest” between strain steps but will not eliminate the problem

## Slide 37: Analysis of LAS results
PART 4:

## Slide 38: Analysis of LAS Results
Analysis is easily carried out using prepared MS Excel spreadsheets

## Slide 39: Analysis of LAS Results
Video

## Slide 40: Summary
Linear Amplitude Sweep is being proposed to address concerns over current specification
  Efficient and practical, uses existing equipment and testing geometry
VECD analysis can be employed to account for traffic and pavement structure

## Slide 41: Thank You!
UWMARC.org
Questions?
Notes: 41